Issue 05/2015

TECHNICAL DATASHEET

SELF-ADHESIVE TAPE WITH PERMANENTLY ELASTIC SEALANT

for securing the critical joints in waterproofing systems

APPLICATION

Self-adhesive tape for securing critical joints in structures. It is applied when installing a waterproofing system, especially in Hidromal, HidromalFleks and AdingFleks, by placing tape on the corners between the layers of the waterproofing system. It is appropriate for repair of waterproofing of surfaces with existing small cracks. It is also applied for covering cracks before rendering and it is used as an air seal.

PROPERTIES

- good adhesion properties to various substrates;

- adjustable;

- the tape is suitable for use with paint, gypsum, cement and adhesives

- durable flexibility;

- easy and precise to apply;

- produces small amount of waste when applied;

- clean and smooth application.

TECHNICAL FEATURES

| FEATURE | VALUE | MEASUREMENT UNIT | METHOD |
| --- | --- | --- | --- |
| Shear adhesion | 12 | N/cm2 | H15 |
| Peel adhesion 90o | 8 | N/cm | H48 |
| Peel adhesion 180o | 9 | N/cm | H41 |
| Density | 1.6 | g/cm3 | H6 |
| Vapour permeability | 0.18 | g/m2/24h/mm | ISO 9932/ BS ISO 15106 |
| Thermal stability | -40 to +90 | oC | - |

METHOD OF APPLICATION

SUBSTRATE PREPARATION

The substrate on which the tape is to be applied should be sound, dry, clean, grease free, dusted and without unstable areas and ice. For cleaning the surface, it is necessary to use isopropanol alcohol (IPA), after which the surface should be allowed to dry. When the self-adhesive tape is to be applied on a porous and crumbly substrate, it is recommended that it is previously primed by applying polyvinyl alcohol (PVA) in order to stabilise and seal the substrate.  The temperature of the substrate on which the self-adhesive tape is to be installed should be in the range between +5˚С and +40˚С.

APPLICATION

The self-adhesive tape is installed by applying it on the substrates that need to be bridged.  At first, the paper should be peeled off from the back side of the tape and it should be applied on the substrate by stamping it.  Additionally, the surface should be treated with a small roller in order to provide good adhesion to the substrate. Then, the same procedure should be repeated with the remaining tape after which the entire length of the joint should be treated with a roller to provide the finish. When applying, it is necessary to pay attention to avoid that the tape comes into contact with small stones and dust in order to maintain the adhesion properties which are necessary for good bonding with the substrate.

PACKAGING

The product is packed in rolls of protective paper with the following dimensions:

| THICKNESS | WIDTH | LENGTH |
| --- | --- | --- |
| 0.8 mm | 7.5 cm | 10 m |
| 0.8 mm | 10 cm | 10 m |
| 0.8 mm | 7.5 cm | 50 m |
| 0.8 mm | 10 cm | 50 m |
| 1.0 mm | 7.5 cm | 10 m |
| 1.0 mm | 10 cm | 10 m |
| 1.0 mm | 7.5 cm | 50 m |
| 1.0 mm | 10 cm | 50 m |

Packaging tolerances:

in width +/- 10%, in length up to 100 mm +/- 2 mm, in  length over 100 mm +/- 3 mm.

STORAGE

The product should be stored in cool and dry premises, placed on a flat surface, in the original packaging.

SHELF LIFE: 24 months.

HAZARD INFORMATION

The product is not classified as hazardous according to Article 31 and Annex 2 of the EU REACH regulation.

PROTECTION

When installing the self-adhesive tape, it is not necessary to have protection of the respiratory system. Usually it is not necessary to wear skin and hand protection. If the product is used frequently or for extended period of time, it is necessary to wear safety gloves. Avoid eye contact.  After application it is required to wash your hands.

IF IN EYES: In case of contact with eyes, rinse immediately with plenty of water. If eye irritation persists: Get medical advice/attention. Rinse immediately with plenty of water for a period of 15 minutes. Remove contact lenses and open the eyes wide. Get medical advice/attention if you feel unwell.

IF ON SKIN: Remove it and wash with soap and water. If irritation occurs, get medical advice/attention.

IF INHALED: Go out into fresh air. If irritation persists, get medical advice/attention.

IF SWALLOWED:  If irritation occurs, get medical advice/attention.

The information provided in this technical datasheet have been obtained through laboratory testing and experiences. The features given are typical and they are not specified. In view of the wide range and variations of substrates, it is recommended that the user tries the product in order to establish if it is suitable for the respective application.